Epoxy resin(水晶膠)

Introduction

Epoxy resin is a kind of unsaturated alkene. It has a faint yellow color and a sticky feel. If an appropriate amount of "hardening agent" (a purple liquid) and "enhancer" (with cobalt soap) is added, chemical reaction occurs. The product formed is a solid with high degree of transparency.  Small objects can be placed into resin before it is solidified (like specimens of small animals, plants, ores, electronic components or coins), resulting in an artistic display.

Procedure

- Estimate the amount of epoxy resin needed.  Measure the required amount of epoxy resin with measuring cylinder.  Wipe the interior of a mold with release agent. Pour the epoxy resin into the mold.

- Use dropper to transfer appropriate amount of hardening agent into the mold. (40 drops of hardening agent are need for each 100mL of epoxy resin. Stir carefully and avoid trapping any air bubble in the mold.

- Add an equal amount of enhancer. Stir thoroughly. Place it aside and wait until it solidifies into semi-solid form.

- Place a small object into the semi-solid mixture. Then wait until it solidifies completely.

- Remove the solidified epoxy resin from the mold.